Control plan when applying cement-based membranes (according to NS-EN 1504-10)

| Tests and checks of the substrate |
| --- |
| Check | Check method | Check scope | Requirements |
| Cleanliness of the substrate | Visual inspection or testing using adhesive tape. | Visual inspection of entire surface. Spot checks may be performed using adhesive tape. | No impurities or residues of surface treatment of the substrate can be accepted. |

| Check upon reception of products and system |
| --- |
| Check | Check method | Check scope | Requirements |
| Identity | Check identity of all products used. | Identity must always be checked before use. | Marking and labels should be in accordance with NS-EN 1504-8, certificate/project description. |

| Tests and checks before and during application |
| --- |
| Check | Check method | Check scope | Requirements |
| Moisture in the substrate | Visual inspection/sampling. Measurement of electrical resistance or RH. | The entire surface should be checked visually before and during application of surface treatment. | Moisture should not exceed 92% (RH). |
| Temp. of substrate | Thermometer. | Continuously during application. Measurements to be recorded once the temperature is stable (< 1 °C/5 minutes) | The temperature must be between +8 and +35 °C. |
| Ambient temp. | Thermometer. | To be performed continuously, and for as long as changes of 2 °C are registered. | The temperature must be between +8 and +35 °C. |
| Ambient humidity | Check and test using a hygrometer. | The measurements should be taken continuously for as long as the works continue. | Ambient humidity (RH) should be ≤ 85%. |
| Precipitation | Visual observation of rain, snow, dew and spray. | The precipitation should be recorded daily for as long as the works continue. | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |
| Wind strength | Check using an anemometer. | The measurements should be taken continuously for as long as the works continue. | The wind strength should be in accordance with the requirements in the project description, …. m/s. |
| Dew point | Check and test using a thermometer and a hygrometer. | The dew point should be checked continuously for as long as the works continue. | The temperature of the substrate should be at least 3 °C higher than the dew point temperature. |
| Wet film thickness | Measure the wet film immediately after application. Each test consists of 3 separate measurements. | The measurements are to be performed in such a way that they provide a representative picture. The scope is selected by the responsible contractor, …. psc / …. m2. | The wet film thickness should be in accordance with the project description, or 3,0 – 4,0 mm. |

| Tests and checks after application |
| --- |
| Check | Check method | Check scope | Requirements |
| Thickness or coverage of repair materials | Check to be performed using a cover meter or by measuring drilled cores. | The check should be performed as a spot check, …. psc / …. m2. | Performed to document fulfilment of the coverage requirement, or 3,0 – 4,0 mm. |
| Coverage of coating | Visual inspection. | The entire surface should be checked. | The coverage of the coating should be in accordance with the project description. There should be no fissures, pores, pinholes or damage to the coating. |
| Adhesion | Extraction of core sample and visual inspection; compressive strength test if necessary. | Tests and checks to be performed in accordance with specified scope, …. psc / …. m2. | Adhesion should be ≥ 1,0 MPa. |
| Colour and structure of finished surface | Check to be performed by visual inspection | The entire surface should be checked. | Colour and structure should be in accordance with the specification. |

Checklist for testing and checking before, during and after application

| Project information | Responsible contractors | Location |  |
| --- | --- | --- | --- |
| Name/designation: |  | Company: |  | Floor, axis, number, etc.: |  |
| Address: |  | Performed by: |  |  |  |
| Contact person: |  | Address: |  |  |  |
| Tel.: |  | Tel.: |  |  |  |
| E-mail: |  | E-mail: |  |  |  |
| Date/time |  |  |  |  |  |

| Tests and checks of the substrate |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Cleanliness of the substrate | No impurities or residues of surface treatment of the substrate can be accepted. |  |  |  |

| Check upon reception of products and system |
| --- |
| Check | Requirements |  |  |
| Identity | Marking and labels should be in accordance with NS-EN 1504-8, certificate/project description. |
| Product |  | Color |  | Date received | Technical data sheet | Batch number | Control of transport documents | Signature |
| Mapelastic |  |  |  |  | Yes | No |  | Yes | No |  |
| Mapelastic Smart |  |  |  |  | Yes | No |  | Yes | No |  |
| Mapelastic Guard |  |  |  |  | Yes | No |  | Yes | No |  |
| Cem-Elastic |  |  |  |  | Yes | No |  | Yes | No |  |

| Tests and checks before and during application |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Moisture in the substrate | Moisture should not exceed 92% (RH). |  |  |  |
| Temp. of substrate | The temperature must be between +8 and +35 °C. |  |  |  |
| Ambient temp. | The temperature must be between +8 and +35 °C. |  |  |  |
| Ambient humidity | Ambient humidity (RH) should be ≤ 85%. |  |  |  |
| Precipitation | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |  |  |  |
| Wind strength | The wind strength should be in accordance with the requirements in the project description, …. m/s. |  |  |  |

| Dew point | The temperature of the substrate should be at least 3 °C higher than the dew point temperature. |  |  |  |
| --- | --- | --- | --- | --- |
| Wet film thickness | The wet film thickness should be in accordance with the project description, or 3,0 – 4,0 mm. |  |  |  |

| Tests and checks after application: |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Thickness or coverage of repair materials | Performed to document fulfilment of the coverage requirement, or 3,0 – 4,0 mm. |  |  |  |
| Coverage of coating | The coverage of the coating should be in accordance with the project description. There should be no fissures, pores, pinholes or damage to the coating. |  |  |  |
| Adhesion | Adhesion should be ≥ 1,0 MPa. |  |  |  |
| Colour and structure of finished surface | Colour and structure should be in accordance with the specification. |  |  |  |

| Reinforcement |
| --- |
| Product | Used | Compatible products |
| Mapenet 150 | Yes | No | Mapelastic, Mapelastic Smart, Mapelastic Guard. |
| Mapetex Sel | Yes | No | Mapelastic Smart. |

| Waterproofing corners, floor/wall joints and construction joints |
| --- |
| Product | Used | Compatible products | Bruksområde |
| Mapeband | Yes | No | Mapelastic, Mapelastic Smart, Mapelastic Guard, Cem-Elastic. | Inside/outside corners and floor/wall joints and construction joints. |
| Mapeband TPE | Yes | No | Mapelastic, Mapelastic Smart, Mapelastic Guard, Cem-Elastic. | Construction joints and cracks with movement. |