Control plan for chemical injection (according to NS-EN 1504-10)

| Test and checks of the substrate |
| --- |
| Check | Check method | Check scope | Requirements |
| Cleanliness of the substrate | Visual inspection or testing using adhesive tape. | Visual inspection of entire surface. Spot checks may be performed using adhesive tape. | No impurities or residues of surface treatment of the substrate can be accepted. |
| Width/depth of fissure | Crack width gauge, core extraction, visual test or ultrasound test. | Scope shall be specified in the project description, ….pcs/m2. | The measurement results determine the selection of materials, …mm. |
| Movement in fissure | Crack gauges in combination with plaster markers. | Scope shall be specified in the project description, …pcs/m2. | The measurement results determine the selection of materials, …mm. |
| Moisture content in substrate / fissure | Visual inspection of fissures and examination of drilled cores. | Scope shall be specified in the project description. Check of core samples to be performed on a spot-check basis. | The measurement results determine the selection of materials, …RH. |
| Temperature of substrate | Thermometer. | Continuously during injection. Measurements to be recorded once the temperature is stable (< 1 °C/5 minutes). | The temperature should be +5 to +30 °C. Mapepoxy BI-R +21 to +30 °C |
| Contaminants in fissure | Sampling and chemical analysis. | Carried out only if contamination is suspected. | There should not normally be contamination in the fissure. |

| Check on reception of products and system: |
| --- |
| Check | Check method | Check scope | Requirements |
| Identity | Check identity of all products used. | Identity must always be checked before use. | Marking and labels should be in accordance with NS-EN 1504-8, certificate/project description. |

| Tests and checks before and during application: |
| --- |
| Check | Check method | Check scope | Requirements |
| Temp. of substrate | Thermometer. | Continuously during application. Measurements to be recorded once the temperature is stable (< 1 °C/5 minutes) | The temperature must be between +5 and +30 °C. Mapepoxy BI-R +21 to +30 °C |
| Ambient temp. | Thermometer. | To be performed continuously, and for as long as changes of 2 °C are registered. | The temperature must be between +5 and +30 °C. Mapepoxy BI-R +21 to +30 °C |
| Precipitation | Visual observation of rain, snow, dew and spray. | The precipitation should be recorded daily for as long as the works continue. | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |
| Injection pressure | A manometer is used to read the injection pressure. | The injection pressure should be checked and recorded continuously for as long as the works continue. | The injection pressure must not be so high that it damages the construction, …Bar |

| Tests and checks after curing: |
| --- |
| Check | Check method | Check scope | Requirements |
| Water permeability | Karsten test. Core and penetration test. | Tests and checks in accordance with specified scope, …pcs./m2. | Water permeability should be in accordance with the project description, ...RH. |
| Fill level of fissures | Sampling and visual inspection/ultrasound tests. | Tests and checks in accordance with specified scope, …pcs/m2. | The fill level should be in accordance with the project description, …%. |
| Adhesion | Extraction of core sample and visual inspection; compressive strength test if necessary. | Tests and checks in accordance with specified scope, … pcs/m2. | The adhesion between the fissure-filling material and the substrate should be in accordance with the project description, …MPa. |

Checklist for test and check before, during and after application

| Project information | Responsible contractor | Location |  |
| --- | --- | --- | --- |
| Name/designation: |  | Company: |  | Floor, axis, number, etc.: |  |
| Address: |  | Performed by: |  |  |  |
| Contact person: |  | Address: |  |  |  |
| Tel.: |  | Tel.: |  |  |  |
| E-mail: |  | E-mail: |  |  |  |
| Date/time: |  | Date/time: |  |  |  |

| Tests and checks of the substrate |
| --- |
| Check | Requirement | Measured result | Unit | Date / time | Sign. |
| Cleanliness of the substrate | No impurities or residues of surface treatment of the substrate can be accepted. |  | (-) |  |  |
| Width/depth of fissure | The measurement results determine the selection of materials, …mm. |  | (mm) |  |  |
| Movement in fissure | The measurement results determine the selection of materials, …mm. |  | (mm) |  |  |
| Moisture content in substrate/fissure | The measurement results determine the selection of materials, …RH. |  | (RH) |  |  |
| Temperature of substrate | The temperature should be +5 to +30 °C. Mapepoxy BI-R +21 to +30 °C |  | (°C) |  |  |
| Contaminants in fissure | There should not normally be contamination in the fissure. |  | (-) |  |  |

| Check upon reception of product and system: |
| --- |
| Check | Requirement |  |  |
| Identity | Marking and labels should be in accordance with NS-EN 1504-8, certificate/project description. |
| Product |  | Code | Date of reception | Technical data sheet | Batchnumber | Transport dokuments checked | Signature |
| Mapepoxy BI |  | U(F1)W(1)(1/2/3/4)(5/30)(0) |  | Yes | No |  | Yes | No |  |
| Mapepoxy BI-R |  | U(F1)W(1)(1/2/3/4)(21/30)(0) |  | Yes | No |  | Yes | No |  |
| Mapepoxy BI-1,8 |  | U(F1)W(2)(1/2/3/4)(5/30)(0) |  | Yes | No |  | Yes | No |  |
| Resfoam 1 KM |  | U(S1)W(8)(1/3)(5/30) |  | Yes | No |  | Yes | No |  |
| Resfoam S |  | U(S1)W(8)(1/3)(5/30) |  | Yes | No |  | Yes | No |  |
| Purgel |  | U(S1)W(8)(1/3)(5/30) |  | Yes | No |  | Yes | No |  |

| Tests and checks before and during application |
| --- |
| Check | Requirement | Measured result | Unit | Date / time | Sign. |
| Temp. of substrate | The temperature must be between +5 and +30 °C. Mapepoxy BI-R +21 to +30 °C |  | (°C) |  |  |
| Ambient temp. | The temperature must be between +5 and +30 °C. Mapepoxy BI-R +21 to +30 °C |  | (°C) |  |  |
| Precipitation | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |  | (mm) |  |  |
| Injection pressure | The injection pressure must not be so high that it damages the construction, …Bar |  | (Bar) |  |  |

| Tests and checks after curing: |
| --- |
| Check | Requirement | Measured result | Unit | Date / time | Sign. |
| Water permeability | Water permeability should be in accordance with the project description, ...RH. |  | (RF) |  |  |
| Fill level of fissures | The fill level should be in accordance with the project description, …%. |  | (mm) |  |  |
| Adhesion | The adhesion between the fissure-filling material and the substrate should be in accordance with the project description, …MPa. |  | (mm) |  |  |

| Hose injection |  |  |  |
| --- | --- | --- | --- |
| Multiple hoses | Yes | No |  |
| Pressure at termination | Yes | No |  |
| Exits | Yes ** | No **) Show with sketch below |  |

| Comments / sketch |  |  |  |
| --- | --- | --- | --- |
| **) Sketch |