Control plan for application of primer for floor screed

| Tests and checks of the substrate |
| --- |
| Check | Check method | Check scope | Requirements |
| Cleanliness of the substrate | Visual inspection or testing using adhesive tape. | Visual inspection of entire surface. Spot checks may be performed using adhesive tape. | No impurities or residues of surface treatment of the substrate can be accepted. |
| Adhesive strength of the substrate | Extraction of core sample and visual inspection; compressive strength test if necessary. | Tests and checks to be performed in accordance with specified scope, …. psc / …. m2. | Adhesion should be in accordance with the requirements in the project description, …. MPa. |

| Check upon reception of products and system |
| --- |
| Check | Check method | Check scope | Requirements |
| Identity | Check identity of all products used. | Identity must always be checked before use. | Marking and labels should be in accordance with the project description. |

| Tests and checks before and during application |
| --- |
| Check | Check method | Check scope | Requirements |
| Moisture in the substrate | Visual inspection/sampling. Measurement of electrical resistance or RH. | The entire surface should be checked visually before and during application of the primer. | Moisture should not exceed 90% (RH). |
| Temp. of substrate | Thermometer. | Continuously during application. Measurements to be recorded at the perimeter and at doors. | The temperature must be: Primer Eco ≥ 5° C Primer G +5 to +35° C Eco Prim T +5 to +35° C Eco Prim Grip +5 to +35° C |
| Ambient temp. | Thermometer. | The measurements should be taken in the middle of the room. | The temperature must be: Primer Eco ≥ 5° C Primer G +5 to +35° C Eco Prim T +5 to +35° C Eco Prim Grip +5 to +35° C |
| Ambient humidity | Check and test using a hygrometer. | To be performed continuously. | Ambient humidity (RH) should be ≤ 85%. |
| Dew point | Check and test using a thermometer and a hygrometer. | The dew point should be checked continuously. | The temperature of the substrate should be at least 3 °C higher than the dew point temperature. |
| Consumption | Control of applied amount of primer | The measurements are to be performed in such a way that they provide a representative picture. The scope is selected by the responsible contractor, …. psc / …. m2. | Consumption should be: Primer Eco 0,10 – 0,15 kg/m2 Primer G 0,08 – 0,15 kg/m2 Eco Prim T 0,20 – 0,35 kg/m2 Eco Prim Grip 0,10 – 0,20 kg/m |

| Tests and checks after application |
| --- |
| Check | Check method | Check scope | Requirements |
| Coverage of coating | Visual inspection. | The entire surface should be checked. | The coverage of the coating should be in accordance with the project description. There should be no fissures, pores, pinholes or damage to the coating. |
| Adhesion | Extraction of core sample and visual inspection; compressive strength test if necessary. | Tests and checks to be performed in accordance with specified scope, …. psc / …. m2. | Adhesion should be in accordance with the requirements in the project description, …. MPa. |

Checklist for testing and checking before, during and after application

| Project information | Responsible contractors | Location |  |
| --- | --- | --- | --- |
| Name/designation: |  | Company: |  | Floor, axis, number, etc.: |  |
| Address: |  | Performed by: |  |  |  |
| Contact person: |  | Address: |  |  |  |
| Tel.: |  | Tel.: |  |  |  |
| E-mail: |  | E-mail: |  |  |  |
| Date/time |  |  |  |  |  |

| Tests and checks of the substrate |
| --- |
| Check | Requirements | Check | Unit | Date / Time | Sign. |
| Cleanliness of the substrate | No impurities or residues of surface treatment of the substrate can be accepted. |  |  |  |  |
| Adhesive strength of the substrate | Adhesion should be in accordance with the requirements in the project description, …. MPa. |  |  |  |  |

| Check upon reception of products and system |
| --- |
| Check | Requirements |  |  |
| Identity | Marking and labels should be in accordance with the project description. |
| Product |  | Color |  | Date received | Technical data sheet | Batch number | Control of transport documents | Signature |
| Primer Eco |  |  |  |  | Yes | No |  | Yes | No |  |
| Primer G |  |  |  |  | Yes | No |  | Yes | No |  |
| Eco Prim T |  |  |  |  | Yes | No |  | Yes | No |  |
| Eco Prim Grip |  |  |  |  | Yes | No |  | Yes | No |  |

| Tests and checks before and during application |
| --- |
| Check | Requirements | Check | Unit | Date / Time | Sign. |
| Moisture in the substrate | Moisture should not exceed 90% (RH). |  |  |  |  |
| Temp. of substrate | The temperature must be: Primer Eco ≥ 5° C Primer G +5 to +35° C Eco Prim T +5 to +35° C Eco Prim Grip +5 to +35° C |  |  |  |  |
| Ambient temp. | The temperature must be: Primer Eco ≥ 5° C Primer G +5 to +35° C Eco Prim T +5 to +35° C Eco Prim Grip +5 to +35° C |  |  |  |  |
| Ambient humidity | Ambient humidity (RH) should be ≤ 85%. |  |  |  |  |
| Dew point | The temperature of the substrate should be at least 3 °C higher than the dew point temperature. |  |  |  |  |

| Consumption | Consumption should be: Primer Eco 0,10 – 0,15 kg/m2 Primer G 0,08 – 0,15 kg/m2 Eco Prim T 0,20 – 0,35 kg/m2 Eco Prim Grip 0,10 – 0,20 kg/m |  |  |  |  |
| --- | --- | --- | --- | --- | --- |

| Tests and checks after application: |
| --- |
| Check | Requirements | Check | Unit | Date / Time | Sign. |
| Coverage of coating | The coverage of the coating should be in accordance with the project description. There should be no fissures, pores, pinholes or damage to the coating. |  |  |  |  |
| Adhesion | Adhesion should be in accordance with the requirements in the project description, …. MPa. |  |  |  |  |