Control plan when applying Silexcolor Paint / Tonachino

| Tests and checks of the substrate |
| --- |
| Check | Check method | Check scope | Requirements |
| Cleanliness of the substrate | Visual inspection or testing using adhesive tape. | Visual inspection of entire surface. Spot checks may be performed using adhesive tape. | No impurities or residues of surface treatment of the substrate can be accepted. |

| Check upon reception of products and system |
| --- |
| Check | Check method | Check scope | Requirements |
| Identity | Check identity of all products used. | Identity must always be checked before use. | Marking and labels should be in accordance with the project description. |

| Tests and checks before and during application |
| --- |
| Check | Check method | Check scope | Requirements |
| Moisture in the substrate | Visual inspection/sampling. Measurement of electrical resistance or RH. | The entire surface should be checked visually before and during application of surface treatment. | Moisture should not exceed 85% (RH). |
| Temp. of substrate | Thermometer. | Continuously during application. Measurements to be recorded once the temperature is stable (< 1 °C/5 minutes) | The temperature must be between +8 and +35 °C. |
| Ambient temp. | Thermometer. | To be performed continuously, and for as long as changes of 2 °C are registered. | The temperature must be between +8 and +35 °C. |
| Ambient humidity | Check and test using a hygrometer. | The measurements should be taken continuously for as long as the works continue. | Ambient humidity (RH) should be ≤ 85%. |
| Precipitation | Visual observation of rain, snow, dew and spray. | The precipitation should be recorded daily for as long as the works continue. | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |
| Wind strength | Check using an anemometer. | The measurements should be taken continuously for as long as the works continue. | The wind strength should be in accordance with the requirements in the project description, …. m/s. |
| Dew point | Check and test using a thermometer and a hygrometer. | The dew point should be checked continuously for as long as the works continue. | A requirement of a dew-free substrate should be specified in the project description or a temperature of at least 5 °C higher than the dew point temperature. |
| Wet film thickness | Measure the wet film immediately after application. Each test consists of 3 separate measurements. | The measurements are to be performed in such a way that they provide a representative picture. The scope is selected by the responsible contractor. | The wet film thickness should be: Silexcolor Paint 0.35–0.45 kg/m² Silexcolor Tonachino 1.70–3.00 kg/m² depending on the graining described. |

| Tests and checks after application |
| --- |
| Check | Check method | Check scope | Requirements |
| Coverage of coating | Visual inspection. | The entire surface should be checked. | The coverage of the coating should be in accordance with the project description or the manufacturer’s instructions. There should be no fissures, pores, pinholes, gaps or damage to the coating. |
| Adhesion | Extraction of core sample and visual inspection; compressive strength test if necessary. | Tests and checks to be performed in accordance with specified scope. | Adhesion should be in accordance with the project description. |
| Colour and structure of finished surface. | Visual inspection. | The entire surface should be checked. | Colour and structure should be in accordance with the specification. |

Checklist for testing and checking before, during and after application

| Project information | Responsible contractors | Location |  |
| --- | --- | --- | --- |
| Name/designation: |  | Company: |  | Floor, axis, number, etc.: |  |
| Address: |  | Performed by: |  |  |  |
| Contact person: |  | Address: |  |  |  |
| Tel.: |  | Tel.: |  |  |  |
| E-mail: |  | E-mail: |  |  |  |
| Date/time |  |  |  |  |  |

| Tests and checks of the substrate |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Cleanliness of the substrate | No impurities or residues of surface treatment of the substrate can be accepted. |  |  |  |

| Check upon reception of products and system |
| --- |
| Check | Requirements |  |  |
| Identity | Marking and labels should be in accordance with the project description. |
| Product |  | Color |  | Date received | Technical data sheet | Batch number | Control of transport documents | Signature |
| Silexcolor Paint |  |  |  |  | Yes | No |  | Yes | No |  |
| Silexcolor Tonachin |  |  |  |  | Yes | No |  | Yes | No |  |

| Tests and checks before and during application |
| --- |
| Check | Requirements | Check | Unit | Date / Time | Sign. |
| Moisture in the substrate | Moisture should not exceed 85% (RH). |  |  |  |
| Temp. of substrate | The temperature must be between +8 and +35 °C. |  |  |  |
| Ambient temp. | The temperature must be between +8 and +35 °C. |  |  |  |
| Ambient humidity | Ambient humidity (RH) should be ≤ 85%. |  |  |  |
| Precipitation | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |  |  |  |
| Wind strength | The wind strength should be in accordance with the requirements in the project description, …. m/s. |  |  |  |

| Dew point | A requirement of a dew-free substrate should be specified in the project description or a temperature of at least 5 °C higher than the dew point temperature. |  |  |  |
| --- | --- | --- | --- | --- |
| Wet film thickness | The wet film thickness should be: Silexcolor Paint 0.35–0.45 kg/m² Silexcolor Tonachino 1.70–3.00 kg/m² depending on the graining described. |  |  |  |

| Tests and checks after application: |
| --- |
| Check | Requirements | Check | Unit | Date / Time | Sign. |
| Coverage of coating | The coverage of the coating should be in accordance with the project description or the manufacturer’s instructions. There should be no fissures, pores, pinholes, gaps or damage to the coating. |  |  |  |  |
| Adhesion | Adhesion should be in accordance with the project description. |  |  |  |  |
| Colour and structure of finished surface. | Colour and structure should be in accordance with the specification. |  |  |  |  |