Control plan for application of Antipluviol W

| Tests and checks of the substrate |
| --- |
| Check | Check method | Check scope | Requirements |
| Cleanliness of the substrate | Visual inspection or testing using adhesive tape. | Visual inspection of entire surface. Spot checks may be performed using adhesive tape. | No impurities or residues of surface treatment of the substrate can be accepted. |

| Check upon reception of products and system |
| --- |
| Check | Check method | Check scope | Requirements |
| Identity | Check identity of all products used. | Identity must always be checked before use. | Marking and labels should be in accordance with project description. |

| Tests and checks before and during application |
| --- |
| Check | Check method | Check scope | Requirements |
| Moisture in the substrate | Visual inspection/sampling. Measurement of electrical resistance or RH. | The entire surface should be checked visually before and during application of surface treatment. | Moisture should not exceed 85%. |
| Temp. of substrate | Thermometer. | Continuously during application. Measurements to be recorded once the temperature is stable (< 1 °C/5 minutes) | The temperature must be between +5 and +35 °C. |
| Ambient temp. | Thermometer. | To be performed continuously, and for as long as changes of 2 °C are registered. | The temperature must be between +5 and +35 °C. |
| Ambient humidity | Check and test using a hygrometer. | The measurements should be taken continuously for as long as the works continue. | Ambient humidity (RH) should be ≤ 85%. |
| Precipitation | Visual observation of rain, snow, dew and spray. | The precipitation should be recorded daily for as long as the works continue. | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |
| Wind strength | Check using an anemometer. | The measurements should be taken continuously for as long as the works continue. | The wind strength should be in accordance with the requirements in the project description, …. m/s. |
| Dew point | Check and test using a thermometer and a hygrometer. | The dew point should be checked continuously for as long as the works continue. | The temperature of the substrate should be at least 3 °C higher than the dew point temperature. |

| Tests and checks after application |
| --- |
| Check | Check method | Check scope | Requirements |
| Depth of penetration of impregnation | Core tests and visual inspection. Concrete cores, normally 60 mm in diameter, should be drilled out. The cores should be marked and split longitudinally. Water should then be applied to the broken surface. Impregnated concrete will not absorb water, whereas the rest of the concrete will absorb water and darken. The depth of penetration is measured as the distance from the surface to the transition between absorbent and non-absorbent concrete. The depth of penetration is specified as a mean value for each broken surface. All broken surfaces should be photographed, with the sample identity visible. | The scope of sampling should be specified in the project description. Sampling should be evenly distributed on all surfaces to provide a representative picture, …. psc / …. m2. | The depth of penetration of hydrophobic impregnation should be specified in the project description, …. m2. |
| Water permeability | Karsten test. Core and penetration test. | Tests and checks to be performed in accordance with specified scope, …. psc / …. m2. | The water permeability should be in accordance with the project description, …. mm. |

Checklist for testing and checking before, during and after application

| Project information | Responsible contractors | Location |  |
| --- | --- | --- | --- |
| Name/designation: |  | Company: |  | Floor, axis, number, etc.: |  |
| Address: |  | Performed by: |  |  |  |
| Contact person: |  | Address: |  |  |  |
| Tel.: |  | Tel.: |  |  |  |
| E-mail: |  | E-mail: |  |  |  |
| Date/time |  |  |  |  |  |

| Tests and checks of the substrate |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Cleanliness of the substrate | No impurities or residues of surface treatment of the substrate can be accepted. |  |  |  |

| Check upon reception of products and system |
| --- |
| Check | Requirements |  |  |
| Identity | Marking and labels should be in accordance with project description. |
| Product |  | Color |  | Date received | Technical data sheet | Batch number | Control of transport documents | Signature |
|  |  |  |  |  | Yes | No |  | Yes | No |  |

| Tests and checks before and during application |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Moisture in the substrate | Moisture should not exceed 85%. |  |  |  |
| Temp. of substrate | The temperature must be between +5 and +35 °C. |  |  |  |
| Ambient temp. | The temperature must be between +5 and +35 °C. |  |  |  |
| Ambient humidity | Ambient humidity (RH) should be ≤ 85%. |  |  |  |
| Precipitation | The precipitation requirements should be specified in the project description. No precipitation directly onto the construction. |  |  |  |
| Wind strength | The wind strength should be in accordance with the requirements in the project description, …. m/s. |  |  |  |

| Dew point | The temperature of the substrate should be at least 3 °C higher than the dew point temperature. |  |  |  |
| --- | --- | --- | --- | --- |

| Tests and checks after application: |
| --- |
| Check | Requirements | Check | Date / Time | Sign. |
| Depth of penetration of impregnation | The depth of penetration of hydrophobic impregnation should be specified in the project description, …. m2. |  |  |  |
| Water permeability | The water permeability should be in accordance with the project description, …. mm. |  |  |  |